产品规格书/Specification

| 产品/product: | 导电铂浆，共烧铂浆/ Pt paste |
| --- | --- |
| 料号/Part number: | 55H-1803 |

适用范围/Application:

此产品适用于高温共烧电极，传感器类产品使用

Suitable for Alumina ceramic products、thick film circuit、sensor electrode.

使用条件/Operating conditions：

| 基材 Substrate | 高温陶瓷 High temperature ceramic |
| --- | --- |
| 印刷 Printing | 200-300目丝网印刷 200-300 mesh screen |
| 流平 Levelling | 5-15min minutes at room temperature 室温下流平5-15分钟（时间根据流平的实际情况决定）。 |
| 干燥 Drying | 通风烘箱烘烤100-150℃，10-15分钟 (烘烤温度低于300℃，可根据烘烤的实际情况决定烘烤时间) 100-150℃ 10-15 min |
| 烧结 Firing Condition | 隧道炉空气气氛下烧结，峰值850~1300℃（推荐值），不少于10分钟。 最低烧成温度可低到800℃，最高耐温可达1400℃ Atmospheric firing in belt furnace with peak time of not less than 10 Minutes at 850~1300℃ |
| Thinner | ST-1000 |

性能/Characteristics：

1. 浆料性能/Paste Characteristics：

| 性能Characteristic |  | 标准Standard | 测试方法及条件 Test method and conditions |
| --- | --- | --- | --- |
| 1 | Fineness | ≤5μm | FOG test |
| 2 | Viscosity | 120-280Pa.s | Brookfield HBT utility cup and spindle (SC4-14/6R), 10rpm, 25±1℃， Brookfield HBT（博利飞）粘度计， 转子SC4-14/6R), 10rpm, 25±1℃ 粘度可根据用户实际需要调节。 |

2. 烧结后特性/Characteristics after firing：

在1烧结条件下，膜厚8-12m Check fired film produced under the conditions specified in 1）, (Film thickness is 8-12m.)

| 特性 Characteristics |  | Standard 标准 | 测试方法和条件 Test method and conditions |
| --- | --- | --- | --- |
| 3 | Resistivity 方阻 | ≤50mΩ/□ | Test pattern 0.6mm×60mm 测试图形0.6mm×60mm |
| 4 | Adhesion strength 附着力 |  | Peel Test: 0.5mmφ Tin plated Cu wire soldered on 2mm×2mm Pad. 0.5mmφ锡浸铜线，焊接面积2mm×2mm Solder: 96.5Sn/0.5Cu Mildly activated flux used. 焊料：96.5Sn/0.5Cu |
|  | Initial 初始附着力 | ≥45.2N |  |
|  | Ageing 老化附着力 | ≥24.6N | Ageing: 150℃×24hrs 老化条件：150℃，24小时 |

保存条件，有效期/Storage condition and Term of validity

产品应在5-25℃的环境温度下密封储存，有效期为产品发货之日起1年。

The product shall be guaranteed for 1 year after shipping date, keep tightly under at 5-25℃

包装方式/Packaging method：

标准包装，1000g/罐, 样品可提供200克小罐包装

Standard package 1000g/can，if you need sample to test, available 200g with small package.